DIAMONDBOND™ TECHNICAL DATA  SHEET

| Clinical Indications | Universal Adhesive Bonding Resin Material - Enamel, Dentin, Resin, Ceramic & Metal Substrates - For : Esthetic Fillings; Class I, II, III, IV, V, Metal-Free Crown& Bridge, Inlays/Onlays, Laminate-Veneers, Implant-Superstructures, Pins, Post/Core, Splints, Ortho-Brackets, Pit&Fissure Sealant & Flowable Cavity Liner/Base. |
| --- | --- |
| Composition | PolyCrystalline Matrix/Synthetic Collagen Primer |
| Mode of Cure | Dual-Cure : Visible Light Cure (Base) + Self/Auto-Cure (Catalyst), Cure - Light, Auto or Dual |
| Delivery System | 3cc & 7cc vials of ; Adhesive - Catalyst(SC) & Base(VLC), Primers A + B & 5g/3cc - Etch Gel. |

| #### PROPERTY ------------------- STD. SPEC. # | #### DIAMOND #### BOND | #### ISO/ADA….. #### Criteria | ** Zinc Phosphate | ##### **Poly-carboxylate | ##### ** Glass Ionomer |
| --- | --- | --- | --- | --- | --- |
| Bond-Strength (MPa) - Dentin 3107(I)/ 8(A)/ 9(A)/(D) | 24 | 5 | 2 | 3 | 8 |
| Bond (MPa) - Enamel 3107(I)/ 8(A)/ 9(A)/(D) | 29 | 7 | 3 | 4 | 6 |
| Bond (MPa) - Composite 3107(I)/ 8(A)/ 9(A)/(D) | 34 | 8 | 3 | 4 | 8 |
| Bond (MPa)- Porcelain 3107(I)/ 8(A)/9(A)/(D) | 30 | 4 | 3 | 4 | 7 |
| Bond (MPa)- Gold Alloys 3107(I)/8(A)/ 9(A)/(D) | 23 | 4 | 4 | 5 | 5 |
| Bond (MPa) - Titanium 3107(I)/8(A)/ 9(A)/(D) | 27 | 5 | 5 | 6 | 7 |
| Bond (MPa) - Chrome-Cobalt 3107(I)/8(A)/ 9(A)/(D | 28 | 5 | 6 | 5 | 7 |
| Fracture Toughness (Kicsr) (MPa m-1/2) 1304(T) | 1.6 | N/A | 0.2 | 0.25 | 0.5 |
| Polymerization Shrinkage(% linear) 4049(I) | 1.1 | N/A | 1.0 | 1.5 | (-) 0.4 |
| VHN Surface Hardness @ 3mm 4049(I) / 27(A) | 93 | 60 | 20 | 30 | 40 |
| Depth of Cure (mm) 4049(I) / 27(A) | 10.2 | 2.0 | N/A | N/A | N/A |
| Film Thickness, Microns (μm) | 5 | 40 | 75 | 50 | 40 |
| Water Sorption (%wt.) (µg/cm3) 4049(I) / 27(A) | 0.7 | 1.7 | > 5 | > 3 | > 8 |
| Cure Kinetics, Tw, Tg, Ts [ Work(w), Gel(g), Set(s) - Time] - Min’ Sec’’ @ 370C 3107(I)/ 8(A)/ 9(A) Self/Auto Cure Mode (Catalyst + Base) (1:1 Ratio) | Tw - 1’30’’ Tg - 2’30’’ Ts - 3’30’’ | 1’00’’minima- 5’00’’maxima- 9’00’’maxima | 1’30’’ 4’00” 8’00” | 1’00’’ 3’00” 7’00” | 1’30’’ 3’00” 8’00” |
| Biocompatability 10993(I) / 41(A) | Excellent | Moderate | Moderate | Moderate | Reactive |
| Catastrophic Strength - Crown / Tooth - Abutment @ OCA(Occlusal Contact Area)(MPa) (D) | 231 | 50 | 50 | 75 | 100 |
| Cytotoxicity (%) 10993(I) / 41(A) | 0 | 40 | 40 | 40 | 60 |
| Resin-Matrix (D) Filler | Crystalline -PEX | N/A | Phosphoric Acid/ Zinc-Phospho-Silicate | Carboxylic acid/ Silicates | Polyacrylic, Carboxylic& Tartaric acids Fl-PAl-Silicates |
| Fluorescent (D) | Yes | N/A | No | No | No |
| Transparent(Clear) / Opaque(White) (D) | Transparent | N/A | Opaque | Opaque | Opaque |
| Synthetic Collagen (D) | Yes | N/A | No | No | No |
| DiamondBond™ Features & Benefits STANDARDS – SPECIFICATION # ISO-4049 ~ 4049(I) ISO-10993 ~ 10993(I) ISO-3107 ~ 3107(I) ADA-27 ~ 27(A) ADA-8 ~ 8(A) ADA-9 ~ 9(A) ADA 41~ 41(A) ASTM 1304 ~ 1304(T) ASTM-ANSI F394-78 ~ F394-78(T) DRM ~ (D) ** ZP(ZincPhosphate), PC(Polycarboxylate, GI(Glass Ionomer) Cements - Bonded to Porcelain Crown * DiamondCrown Cemented w/ DiamondLink Cement & DiamondBond Adhesive | - Cyclic Fatigue Resistant, High Fracture Toughness, Shock Absorbing - Exceptional Bond Strength(Tensile/Shear) and Integration for Maximum Adhesion to Multiple Substrates: Dentin/Enamel/Composite/Ceramic/Alloys - Mimics the properties of Natural tooth Dentition, Synthetic Collagen Polypeptide Bond - Delivers Long Lasting Superior Adhesion, both Bio-Chemical and Physico-Mechanical to Tooth Structure for Ultimate Longevity: Negligible Sorption & Absence of Solubility - Ultra Low Film Thickness ; Tough & Thin Interface for Optimum Crown/Abutment Tooth Fit Integrity and/or Filling/Tooth Marginal Seal (Micro-Elastic) - Crown/Filling Superstucture Reinforcement thru Interfacial Bonding/Substrate Integration - Excellent Marginal Integrity, Low Shrinkage-Low Probability of Post-Operative Sensitivity Microgap / Microleakage/ Microbial Invasion - Free - Superb Color Stability, Stain Resistance and Accurate Esthetic Shade Match - Easy Access, infiltrates the Most Difficult Preps., Enhanced Contact Angle Wetability / Adaptation to Acute Transitional Prep. Line Angles - Delivery Systems, avail. In 3/ 7 cc Primers & Adhesives (Dual-Cure); Visible Light &/or Auto-Cure for both Direct Fillings and Crown & Bridge Application. - Refractive-Index, Chameleon-Like Effect - Biocompatible & Non-Cytotoxic |  |  |  |  |