DIAMONDCROWN™ CHAIRSIDE TECHNICAL DATA  SHEET

| Clinical Indications | Esthetic Class - I, II, III, IV, V Restorations, Chairside Direct/Indirect Prosthodontic Material, Inlays/Onlays and Laminate-Veneers, Metal-Free Crowns and Porcelain Fracture Repairs. |
| --- | --- |
| Mode of Application | Stratification Technique: Op. Dentin-Dentin-Enamel-Incisal |
| Mode of Cure | Visible Light Cure (VLC) |
| Composition | PolyCrystalline NanoCeram |
| Delivery System | 5g. Syringe |

| #### PROPERTY ------------------- STD. SPEC. # | #### DIAMOND #### CROWN | #### ISO/ADA….. #### Criteria | Tooth Enamel/Dentin | ##### Gold | ##### Porcelain |
| --- | --- | --- | --- | --- | --- |
| Diametral Tensile Strength (MPa) 4049(I) / 27(A) | 79 | 34 | 70 | N/A | 35 |
| Biaxial Flexural Strength (MPa) 4049(I) / F394-78(T) | 231 | 52 | 145 | 186 | 68 |
| Compressive Strength (MPa) 4049(I) / 27(A) | 552 | N/A | 393/290 | 166 | 379 |
| Fracture Toughness (Kicsr) (MPa m-1/2) 1304(T) | 2.2 | N/A | 1.7 | 2.2 | 0.5 |
| Wear Resistance (µm/year) 4049(I)/(C)/ (D) | 3 | 50 | 3-5 | 3-5 | “ wears opposing dentition “ |
| Water Sorption (%wt.) (µg/cm3) 4049(I) / 27(A) | 0.25 | 0.70 | N/A | N/A | N/A |
| Polymerization Shrinkage (% linear) 4049(I) | 0.20 | N/A | ------ | 1.56 | 17 |
| Linear Coefficient Thermal Expansion LCTE - (ppm) (mm/mm/0C x 10-6) (D) | 15 | N/A | 11.4 | 14.2 | 14 |
| Ra - Profilometry Average Surface Roughness (nm) (D) | 3 | N/A | 5 | 15 | 15 |
| VHN Surface Hardness @ 3mm 4049(I) / 27(A) | 110 | 60 | 210/80 | 80 | 475 |
| Depth of Cure (mm) 4049(I) / 27(A) | 5.5 | 2.0 | N/A | N/A | N/A |
| Biocompatability 10993(I) / 41(A) | Excellent | Moderate | ------ | Excellent | Moderate |
| Cytotoxicity (%) 10993(I) / 41(A) | 0 | 40 | ------ | 0 | 25 |
| Polishability (D) | Very Good | N/A | Very Good | Very Good | “ N/A-Glazed “ |
| Shades (Vita) (V) | 92 Vita | N/A | ------ | 1 | Vita |
| Particle Size Microns(μm), Nano (nm) (D) | 0.25-0.60 μm (+) 7 nm | N/A | ------ | N/A | N/A |
| Filler Weight (%), Fw (D) | 80.0 | 50.0 | ------ | ----- | ----- |
| Filler Volume (%), Vf (D) | 74.0 | 30.0 | ------ | ----- | ----- |
| Resin / Matrix (D) [Radiopaque, (X-Ray detectable) & Fluorescent] | Crystalline - PEX | N/A | Crystalline - HA | ----- | ----- |
| DiamondCrown™ Chairside Features & Benefits STANDARDS – SPECIFICATION # ISO-4049 ~ 4049(I) ISO-10993 ~ 10993(I) ADA-27 ~ 27(A) ADA 41~ 41(A) ASTM 1304 ~ 1304(T) ASTM-ANSI F394-78 ~ F394-78(T) VITA SHADE ~ (V) CDA ~ (C) DRM ~ (D) | - Cyclic Fatigue Resistant, High Fracture Toughness, Shock Absorbing - Exceptional Fracture Resistance: Tensile, Shear, Compressive & Flexural. - Wear Resistance Similar to Natural Tooth - Easy to Augment Intraorally due to Bond-Strength, 27 MPa - Ideal for Occlusal Rehabilitation(TMJ Syndrome, Bruxers/Habitual Clenchers) - Allows for Immediate Loading of Integrated Implant Permanent Crown Superstructures and Accelerated Osseo-integration due to Tough, Ductile, Shock-Absorbing Characteristics which Dissipates Masticatory Energy. - Ultimate Reinforcement and Handling Characteristics - Thixotropic(Shape-Memory, Anti-Slumping Properties) Easy to Model, Carve, Shape and Anatomically Contour - Modeling Liquid, Ceramo-Coupler & Metal Coupler Facilitates/Diversifies Application Modalities - Superb Color Stability and Accurate Shade Match - Wide Spectrum of Colors(92): Vita A1-D4 Metal Opaques(17), Op. Dentin(16), Dentin(16), Enamel(16), Incisal(6), Dentin Chroma Modifiers(4), Dentin Color Intensifiers(10), Neutral SuperWhite (5) - XXL, XL,L,M,OP, Glaze(1), SuperClear-Coat(1) - Refractive-Index, Chameleon-Like Effect - Specular Reflectance, Gloss & Luster Value - Ultimate Longevity; Negligible Sorption, Absence of Solubility - Excellent Marginal Integrity, Low Shrinkage - Breakthrough Metal Coupling Chemistry Produces Stable Bond to Nickel, Chrome, Gold, Palladium, Zirconium & Titanium - Biocompatible & Non-Cytotoxic |  |  |  |  |