# DRM LABORATORIES, INC.

# DIAMONDLITE(

Universal Direct Dental Restorative Micro-Hybrid Composite - Anterior / Posterior Filling System.

# Visible Light Cure

+

# DIAMONDBOND(

# Universal Dental Adhesive System  (  Dual - Cure

Enamel, Dentin, Metal and Ceramic

Visible Light Cure / Self Cure

-------------------------------------------------------------------------------------------------------------------------------

- Recommended for class I, II, III, IV, V and esthetic direct veneer restorations.

- Store at or below room temperature.

- Keep refrigerated to prolong shelf-life.

# PRECAUTIONARY REMARKS:

# AVOID THE FOLLOWING AGENTS / TECHNIQUES:

- Pumice containing oil or fluoride.

- Hemostatic agent ( Hemodent) containing Ferric Sulfate and / or Aluminum Chloride.

- Retraction cords impregnated with hemostatic agents containing Ferric Sulfate

and / or Aluminum Chloride.

- Thin retraction cords may lead to crevicular fluid hydrostatic flow and cervical

restorative site contamination throughout adhesive, composite placement process.

- Overcuring restorative may lead to post - operative sensitivity.

- Undercuring restorative, i.e; 20 sec. or less per layer and / or use of  VLC apparatus

generating less than 500 mW/cm2 at 450-550 nm wavelength band.

- Moisture or oil containing compressed air contamination.

-------------------------------------------------------------------------------------------------------------------------------

# Alcohol cleanse all instruments, mandrels, etc. to avoid multi- components cross - contamination.

# PREPARATION: USE CONSERVATIVE TOOTH PREPARATION METHODOLOGY:

- Rounded internal line angles, avoid sharp transitions - binding sites.

- Convergent axial walls.

- Smooth cavity floor.

- Do not bevel the occlusal margins.

- Chamfer  the interproximal gingival seat margin.

- Avoid diatoric forms, undercuts, channeling - mechanical retention methods.

# PREPARATION TECHNIQUE:

(Prepare the restorative site.

(Clean with plain pumice, rinse and dry.

(Isolate with rubber dam, or  cotton rolls and thick plain non-impregnated retraction cord, wedge & secure with tooth matrix of choice as needed.

# CONDITIONING, PRIMING & BONDING

# STEP 1 : Conditioning

# ENAMEL & DENTIN

- Apply the DiamondLite( Tooth Conditioning Gel, secure disposable luer lock needle tips onto the 37% orthophosphoric acid gel, place on enamel and dentin surfaces when needed.  Allow to react for 15 seconds while agitating gel with disposable brush tip / brush holder provided (avoid desiccation).

- Stepwise conditioning gel placement is ideal, start with enamel, and at the 15 sec. mark, place gel

on dentin, at the 30 sec. mark from baseline, remove

- Rinse and dry.

# STEP 2: Priming

# DENTIN

- Place 1:1 ratio of  DiamondBond( Primer A & B into well tray, mix with the disposable brush tip /

holder provided and brush several consecutive coats ( 4-6) onto dentin surfaces.

- Apply a gentle jet of air, glossy surface texture.

# STEP 3: Bonding

# ENAMEL AND DENTIN

# VISIBLE LIGHT CURE METHOD

- Place 1 drop of DiamondBond( Universal Adhesive Resin BASE  into a clean well tray provided.

( Place a thin layer of  DiamondBond BASE Adhesive Resin onto both the enamel & dentin with

a disposable brush tip / holder.

- Thin with a jet of air.

- Visible light curing for 30 seconds.

# SELF CURE METHOD

- Place 1 : 1 ratio ( 1 drop of each) of  DiamondBond( Universal Adhesive Resin CATALYST  and

BASE  into a clean well tray provided.

- Mix with a fresh brush tip / holder in well tray for 10 seconds.

- Brush a thin layer of adhesive mixture onto enamel and dentin.

- Thin with jet of air.

- Allow 2.5 minutes to set.

# DUAL CURE METHOD

- Follow self cure instructions.

- Complete cure by visible light for 30 seconds.

# CERAMIC REPAIR SITE

# STEP 1

(Prep. repair surface with diamond bur.

(   Intraoral microsandblast with fine abrasive, the restorative site, or roughen with fine diamond

bur.

(Rinse and dry.

# STEP 2

- Dispense a drop of DiamondLite( Ceramo-Coupler into clean well tray provided.

- Brush a few (2-3) layers of DiamondLite( Ceramo-Coupler onto sandblasted/abraded, cleaned

and dried ceramo-repair site.

- Dry with gentle air jet.

# STEP 3

- Proceed with DiamondBond( Universal Adhesive Resin Layer Placement & follow;

a)  VLC method, or

b)  Self-cure method, or

c)  Dual-cure method

# STEP 4

# FILLING RESTORATIVE SITE

- Select the appropriate shade equivalent syringe of DiamondLite(  Filling Material.

- Apply a layering technique bucco-Lingual (posterior) or stepwise increments (anterior)

light shades - up to 3.0 mm Layers.

- Dark shades - up to 2.0 mm Layers.

- Pat & condense, carve and contour using gentle pressure with the DRM stainless placement instrument provided.

- Avoid porosity inclusions.

- Visible light cure for 40 seconds per layer from each tooth aspect; buccal / facial, lingual, occlusal /

incisal and interproximal ( clear light propagating tooth wedges recommended).

(Remove mylar strips, tooth matrix, crown clear form, cervical clear bands.

# TRIMMING, FINISHING & POLISHING - DIAMONDLITE(

- Trim DiamondLite( with 8-12 fluted carbides, fine diamonds, or white stones.

- Finish with 30 - fine fluted carbides.

- Polish with DiamondLite( Polishing Discs secured onto mandrel provided ( safe-side; allows

interproximal access, pliable texture; allows flexible contouring, with the DiamondLite(

Polishing  Paste.

- For Lingual grooves, occlusal developmental grooves, pits & fissures, gain access with soft bristle

brush wheels, cups or soft rubber; discs, cups, cones or points.

DRM Research Laboratories, Inc. 29 Business Park Drive, Branford, CT  06405

Tel. (203) 488 - 5555 ( Toll Free (888) DRM-BOND [376-2663] ( Fax. (203) 488-2821

( Email drmbond@drmco.com

415-13 Rev B                                                                                                                                    ver. 052510