DIAMONDLITE™ TECHNICAL DATA  SHEET

| Clinical Indications | Universal-Anterior/Posterior Esthetic Filling Material, Class - I, II, III, IV & Direct Laminate-Veneers |
| --- | --- |
| Composition | PolyCrystalline NanoCeram |
| Mode of Cure | Visible Light Cure (VLC) |
| Delivery System | 5g. Syringe & 0.25g Indi-Dose Carpule (x) 20 / Canister |

| PROPERTY ------------------- STD. SPEC. # | DIAMONDLITE |
| --- | --- |

ISO/ADA…..

| Criteria | Tooth Enamel/Dentin | Gold | Porcelain |
| --- | --- | --- | --- |
| Diametral Tensile Strength (MPa) 4049(I) / 27(A) | 64 | 34 | 70 | N/A | 35 |
| Biaxial Flexural Strength (MPa) 4049(I) / F394-78(T) | 198 | 52 | 145 | 186 | 68 |
| Compressive Strength (MPa) 4049(I) / 27(A) | 436 | N/A | 393/290 | 166 | 379 |
| Fracture Toughness (Kicsr) (MPa m-1/2) 1304(T) | 1.65 | N/A | 1.7 | 2.2 | 0.5 |
| Wear Resistance (µm/year) 4049(I)/(C)/ (D) | 7 | 50 | 3-5 | 3-5 | “ wears opposing dentition “ |
| Water Sorption (%wt.) (µg/cm3) 4049(I) / 27(A) | 0.40 | 0.70 | N/A | N/A | N/A |
| Polymerization Shrinkage(% linear) N 4049(I) | 0.50 | N/A | ------ | 1.56 | 17 |

Linear Coefficient Thermal Expansion

LCTE - (ppm) (mm/mm/0C x 10-6) (D)

20

N/A

11.4

14.2

14

Ra-Profilometry Average Surface Roughness (nm)(D)

15

N/A

5

15

| 15 |
| --- |
| VHN Surface Hardness @ 3mm 4049(I) / 27(A) | 100 | 60 | 210/80 | 80 | 475 |
| Depth of Cure (mm) 4049(I) / 27(A) | 4.2 | 2.0 | N/A | N/A | N/A |
| Biocompatability 10993(I) / 41(A) | Excellent | Moderate | ------ | Excellent | Moderate |
| Cytotoxicity (%) 10993(I) / 41(A) | 0 | 40 | ------ | 0 | 25 |
| Polishability (D) | Very Good | N/A | Very Good | Very Good | “ N/A-Glazed “ |
| Shades (Vita) (V) | 20 Vita | N/A | ------ | 1 | Vita |

Particle Size

| Microns (ìm), Nano (nm) (D) | 0.60 ìm (+) 7 nm | N/A | ------ | N/A | N/A |
| --- | --- | --- | --- | --- | --- |
| Filler Weight (%), Fw (D) | 80.0 | 50.0 | ------ | ----- | ----- |
| Filler Volume (%), Vf (D) | 73.0 | 30.0 | ------ | ----- | ----- |

Resin / Matrix                                                         (D)

| [Radiopaque, (X-Ray detectable) & Fluorescent] | Crystalline - PEX | N/A | Crystalline - HA | ----- | ----- |
| --- | --- | --- | --- | --- | --- |

DiamondLite™

Features & Benefits

STANDARDS – SPECIFICATION #

ISO-4049 ~ 4049(I)

ISO-10993 ~ 10993(I)

ADA-27 ~ 27(A)

ADA 41~ 41(A)

ASTM 1304 ~ 1304(T)

ASTM-ANSI F394-78 ~ F394-78(T)

VITA SHADE ~ (V)

CDA ~ (C)

DRM ~ (D)

Cyclic Fatigue Resistant, High Fracture Toughness, Shock Absorbing

Exceptional Fracture Resistance:  Tensile, Shear, Compressive & Flexural.

Wear Resistance Similar to Natural Tooth

Ultimate Reinforcement and Handling Characteristics

Thixotropic(Shape-Memory, Anti-Slumping Properties) Easy to Model, Carve, Shape and Anatomically Contour

Superb Color Stability and Accurate Shade Match

Wide Spectrum of Colors(20):  Vita A1-D4(16) & SuperBrite(4)-XL,L,M,OP

Delivery Systems, available in both Syringes & Indi-Dose Carpules

Refractive-Index, Chameleon-Like Effect

Specular Reflectance, Gloss & Luster Value

Ultimate Longevity;  Negligible Sorption, Absence of Solubility

Excellent Marginal Integrity, Low Shrinkage

Biocompatible & Non-Cytotoxic