1/3

DIAMONDCROWN (Metal-Free) PROSTHODONTICS – CEMENTATION PROTOCOL

- INLAY / ONLAY / CROWN & BRIDGE / LAMINATE-VENEERS (w/ Inciso-lingual wrap)

DUAL-CURE

1)  Remove Temporary Filling Material/Crown.

2)  Pumice w/ plain flour of pumice (fluoride and oil-free).

3)  Etch Tooth/Abutment surface, Enamel and Dentin, 15-20 s., rinse and dry w/ compressed air (oil and

moisture-free).

4)  Isolate Prep./Sulcus w/ Retraction Cord(non-impregnated, #8 gauge), to avoid Crevicular fluid

Contamination during bonding/cementation procedure, Molar Mylar Matrix, Trans-Illuminating wedges and

Cotton rolls. (Rubber Dam only is insufficient isolation during bonding/cementation protocol)

5)  DiamondCrown internal surface - clean w/ 95% denatured Ethanol (Ethyl Alcohol) w/ disposable brush tip

and air dry w/ compressed air.

6)  Dispense a drop of DiamondBond Ceramo-Coupler into a disposable well, brush 2-3 layers w/ a disposable

brush onto the internal surface of the DiamondCrown, jet-dry gently w/ compressed air.

7)  Dispense 1 drop of each DiamondBond-001 Universal Adhesive Bonding Agent - Catalyst + Base (Dual-

Cure), mix for 10 s. in a disposable well and brush 2-3 layers onto the Etched Enamel and Dentin tooth

prep. surface and the internal surface of the Ceramo-Coupler coated DiamondCrown, jet air dry gently for

5 s. both the tooth abutment surface and the internal aspect of the Crown.

Caution:  Do not Light Cure at this juncture.

7a) Alternatively, Dispense 1 drop of each DiamondBond  Primer A + B mix for 10 s. in a disposable well and

brush 2-3 layers onto the Dentin tooth prep. surface, jet air dry gently w/ compressed air for 5 s.

Then, Dispense 1 drop of each DiamondBond (Original) Universal Adhesive Bonding Agent - Catalyst +

Base (Dual-Cure), mix for 10 s. in a disposable well and brush 2-3 layers onto the Etched Enamel and

Primed Dentin tooth prep. surface and the internal surface of the Ceramo-Coupler coated DiamondCrown,

gently thin-out  w/ a jet of air for 5 s. both the tooth abutment surface and the internal aspect of the Crown.

Caution:  Do not Light Cure at this juncture.

8)  Mix 1:1 ratio of DiamondLink 2-F/C Cement - Catalyst + Base (of the appropriate shade: B1-Translusent, or

A2-Natural, or B3-Yellow), on a clean and dry Glass slab w/ a #324 Stainless Steel Spatula for 15 s. until a

Uniform/homogenous mix is attained (spread and envelope the mix onto glass slab as to avoid micro-

porosities, do not swirl).  Place an Aliquot of the mixture centrally in the DiamondCrown internal aspect (do

not flood the Crown shell, this will only lead to an excessive amount of cement expectorating upon the

sitting of the Crown.  A small aliquot of the mix is sufficient, it will coat the entire internal aspect by

capillary-flow action).  Sit the Crown onto the Tooth Abutment, apply central/equilibrated digital pressure,

allow excess to exude.

2/3

Sweep the VLC Light Curing Probe around the margin for 2-3 s. (that will semi-gel the excess), remove

excess w/ a blunt instrument.  Allow 1.5 min. for the Auto-Cure reaction to take place and Trans-illuminate

thru the Crown for 16 s. w/ the DiamondLED-Mini Curing Probe from each tooth aspect.

9)  Remove the isolation devices, polish the Inter-proximal / margins w/ Esthetic sanding strips (Fine followed

by Super-Fine only).  Clear Inter-proximal /margins w/ Floss (check for any potential slight overhang  from

excessive cement exudate, repeat polishing and clearance). Articulate, adjust the bite and polish w/

Ultra-fine Silicone points/cups/wheels(Diamond-Polishers-Hybrid-Class) followed by Nylon Bristle Soft

Brush Cups + DiamondLite Polishing Paste @ slow-speed.

- LAMINATE-VENEERS (facial surface coverage only)

VISIBLE LIGHT CURE

1)  Remove Temporary Material

2)  Pumice w/ plain flour of pumice (fluoride and oil-free).

3)  Etch Tooth prep.surface, Enamel 20 s., rinse and dry w/ compressed air (oil and moisture-free).

4)  Isolate Prep./Sulcus w/ Retraction Cord(non-impregnated, #8 gauge), to avoid Crevicular fluid

Contamination during bonding/cementation procedure, Cervical Mylar Matrix, Trans-Illuminating wedges

and Cotton rolls. (Rubber Dam only is insufficient isolation during bonding/cementation protocol)

5)  DiamondCrown Laminate internal surface - clean w/ 95% denatured Ethanol (Ethyl Alcohol) w/ disposable

brush tip and air dry w/ compressed air.

6)  Dispense a drop of DiamondBond Ceramo-Coupler into a disposable well, brush 2-3 layers w/ a disposable

brush onto the internal surface of the DiamondCrown Laminate, jet-dry gently w/ compressed air.

7)  Dispense 1 drop of each DiamondBond-001 Universal Adhesive Bonding Agent - Base (VLC) in a

disposable well and brush 2-3 layers onto the Etched Enamel tooth prep. surface and the internal surface

of the  Ceramo-Coupler coated DiamondCrown Laminate, jet air dry gently for 5 s. both the tooth prep.

surface and the internal aspect of the Crown.

Caution:  Do not Light Cure at this juncture.

7a) Alternatively, dispense 1 drop of each DiamondBond (Original) Universal Adhesive Bonding Agent -

Base (VLC) in a disposable well and brush 2-3 layers onto the Etched Enamel tooth prep. surface and

the internal surface of the Ceramo-Coupler coated DiamondCrown Laminate, gently thin-out  w/ a jet of air

for 5 s.both the tooth prep. surface and the internal aspect of the DiamondCrown Laminate.

Caution:  Do not Light Cure at this juncture.

8)  Dispense a small amount of DiamondLink 2-F/C Cement - Base (VLC) (of the appropriate shade: B1-

Translusent, or A2-Natural, or B3-Yellow), on a clean and dry Glass slab w/ a #324 Stainless Steel Spatula.

Place an Aliquot of the mixture centrally in the DiamondCrown Laminate internal aspect (do not flood the

Venner shell, this will only lead to an excessive amount of cement expectorating upon the sitting of the

Laminate.  A small aliquot of the mix is sufficient, it will coat the entire internal aspect by capillary-flow

3/3

action). Sit the Laminate-Veneer onto the Tooth Prep. surface, apply central/equilibrated digital pressure,

allow excess to exude.  Sweep the VLC Light Curing Probe around the margin for 2-3 s. (that will semi-gel

the excess), remove excess w/ a blunt instrument.  Trans-illuminate thru the DiamondCrown Laminate-

Veneer for 16 s. w/ the DiamondLED-Mini Curing Probe from each tooth aspect.

9)  Remove the isolation devices, polish the Inter-proximal / margins w/ Esthetic sanding strips (Fine followed

by Super-Fine only).  Clear Inter-proximal /margins w/ Floss (check for any potential slight overhang  from

excessive cement, repeat polishing and clearance). Articulate, adjust the bite and polish w/ Ultra-fine

Silicone points/cups/wheels (Diamond-Polishers-Hybrid-Class) followed by Nylon Bristle Soft Brush Cups

+ DiamondLite Polishing Paste @ slow-speed.